Mixing Concrete
someonesdad1@gmail.com 12 Jan 2014 Updated 11 Mar 2023
A relatively common homeowner task is mixing up a small amount of concrete for a yard project. There are three common ways of doing this:
- Using bags of premix
- Mixing the component materials yourself
- Have a truck deliver your order or pulling a trailer of concrete home
We'll ignore the last way, as you can consult with the folks you buy the stuff from.
The package concrete.zip includes a python script concrete.py which will help with the calculations of quantities of the needed raw materials to get a desired finished volume of concrete, in a few common shapes. I wrote this script to 1) help me deal with the screwball US units customarily used for both volume and lengths and 2) to remember the proper proportions and water quantities to use.
All density (specific gravity) numbers in this document are in g/mL. Multiply by 1000 to get kg/m3 and 62.4 to get lbm/ft3.
Don't confuse the terms cement and concrete. In casual use, they mean the same thing, but cement technically refers to Portland cement, a powder that is a component of concrete. Concrete is a mixture of cement, sand, gravel, and water (and is often reinforced by steel wire/bars).
An 80 lb bag of premix winds up giving you 0.6 ft3 of concrete. Since concrete is about 150 lbs/ft3, this means you get 90 lb of concrete.
# Algorithm for making concrete
There are numerous references on the web. The one in [memph] is pretty good and is the basis of what's given here. Civil engineering courses go into lots of detail about how to properly mix concrete. For us (the typical homeowner), it's reasonable to fall back on the rule of thumb that concrete's components should be mixed in the ratio of 1:2:3, which indicates the mass proportions of the cement : sand : gravel (aggregate). You will also see ratios such as 1:2:2 and 1:2:4.
[glover] gives the density of cured concrete with gravel as 2.5 g/cc (156 lbm/ft3). Reinforced concrete has a density of about 2.2 g/cc (137 lbm/ft3).
## Algorithm for component amounts
We'll use the following symbols. Be sure to use a consistent set of units. The subscript c denotes cement, s sand, and g gravel.
alignl stack { V_0 `=` "desired volume of cured concrete" # V `=` "volume of mixed dry components" `=` %mu V_0 # %alpha `=` "water to cement mass ratio" # %mu `=` "\"make sure you have enough\" factor (a number a bit above 1)" # %rho_0 `=` "density of cured concrete" # %rho_x `=` "density of component x" # %beta_x `=` "component fraction of x" }
The algorithm for calculating the mass or volume of the required components is:
1. Determine the volume V0 of cured concrete needed.
2. Calculate V `=` %mu V_0 to get the required volume of mixed dry components.
3. Calculate M `=` %rho_0 V , which is the mass of concrete you'll mix.
4. Using the recommended component proportions, calculate the mass of the components needed.
  1. m_c `=` "mass of cement" `=` %beta_c M
  2. m_s `=` "mass of sand" `=` %beta_s M
  3. m_g `=` "mass of gravel" `=` %beta_g M
5. Calculate the mass of water needed as m_w `=` %alpha M .
  1. The total mass of concrete you mix should be near m_c + m_s + m_g + m_w . A little of the water will be lost to evaporation over time, so this is only an approximation. The minimum mass can be calculated by using the stoichiometric value of  of 0.25.
6. If you are unable to measure the mass of the components, convert them to volumes:
  1. v_c `=` "volume of cement" `=` m_c/%rho_c
  2. v_s `=` "volume of sand" `=` m_s/%rho_s
  3. v_g `=` "volume of gravel" `=` m_g/%rho_g
  4. v_w `=` "volume of water" `=` m_w/%rho_w
The page http://en.wikipedia.org/wiki/Types_of_concrete#Modern_concrete states that the typical batch of concrete is mixed in the mass (not volume) proportions of 1 part Portland cement, 2 parts dry sand, 3 parts dry stone, and 1/2 part water. They then give the example of 1 cubic foot of concrete being made by using 22 lb of cement, 10 lb water, 41 lb dry sand, and 70 lb of dry stone (1/2" to 3/4" rocks). The resulting concrete would weigh about 143 lb, which is what the components' mass sum to. Note the water/cement mass ratio is 0.45.
## Details
In this section, we look at some of the details in the above algorithm.
### μ: "make sure you have enough" factor
This factor is used to help make sure you make enough concrete in a batch. Making 10% too much is preferable to making 10% too little. You can dump the extra 10% in a pile and toss it when it's hardened. Being 10% too low can make you rush to mix the extra 10% and, if not timely, can result in a poor bond between the two pours.
If you can measure your components by mass, you can make the μ factor smaller than if you work by volume. However, as mentioned, most of us homeowners have to work with volumes because we don't have suitable tools to measure the mass.
## Mixing algorithm
There are three typical methods homeowners use for mixing concrete:
1. Mix in a wheelbarrow.
2. Mix on a chunk of plywood.
3. Mix in a motorized concrete mixer.
I've also mixed a fair bit of concrete in a 5 gallon bucket when I need to put in a fence post or two, but this is a physically brutal thing to do, as it takes quite a bit of effort to get the concrete mixed, avoid dry pockets, and try to hold the bucket still while you're mixing. You might want to build a simple frame to hold the bucket firmly at an angle to make it easier to mix. Use a square shovel or it will be nearly impossible to get all the dry concrete mixed. Put half of the water in the bucket, then add the premix. Getting a good mix in a bucket in a timely fashion is aerobic exercise.
Using a wheelbarrow or a chunk of plywood are both suitable methods. Using plywood usually means constructing a "volcano" from the premix, then smashing it a bit and making a depression in the top. The water is added to the depression and the mix is carefully mixed with the water with a hoe or shovel. If mixing in a wheelbarrow, it's best to use a hoe and ensure the wheelbarrow has a flat bottom. However, realize that mixing concrete by hand is for young people, as it can be a lot of physical work (and you'll probably feel it in your back and arms).
If you have to do a fair bit of concrete mixing, you can buy an electric mixer such as one from Harbor Freight for a few hundred dollars:
The design has been unchanged for the past couple of decades. The only disadvantages are that it's a poor design for manually moving because it's not counterbalanced and the horizontal pipe below the drum gets covered in concrete when you dump into a wheel barrow. However, if you have to mix 20-30 bags of concrete, you'll find the mixer saves you a lot of physical effort.
The mixer is labeled as a 3.5 cubic feet mixer, but since wet concrete has a density of around 2.4 g/mL, you'd be looking at a load of over 500 lbm in the mixer. The marketing idiot who gave this spec never had to mix that much concrete in it. A typical 90 lbm bag of concrete produces about 0.8 cubic feet of concrete and I've mixed up to two of these bags at once. I usually use the 60 lbm bags because they are easier to handle and they give about 0.6 cubic feet.
The following two algorithms are intended for use with a powered mixer. The set-up tasks to perform before starting are:
1. Make sure the mixer is clean, level, and mechanically stable.
2. Make sure you've reviewed the safety information in the mixer's manual.
3. Use the proper extension cord for electrical power.
4. Verify the mixer works and that the tilting mechanism is functional.
### Premix
1. Add half of the needed water for the mix.
2. Pour in the premix.
3. Start the mixer turning.
4. Stop and inspect frequently to ensure you don't have clumps of dry premix sticking to the chamber or mixing paddles. Use a stick or trowel to scrape off any found.
5. When the mix appears uniform and there's no remaining dry material, add the remaining water.
6. Mix for a few minutes until consistent.
7. Pour into container and transport to forms.
8. Clean out the mixing chamber.
The cleaning step is quite important, as it will be quite difficult to get dried concrete off the chamber and paddles (its grip is tenacious and you'll probably damage the mixer trying to get it off). It's best to head this problem off at the pass.
You will be tempted to dump in a bag of premix, start the mixer turning, then spray in water from the hose (this is how I often use premix). Be aware that you almost certainly will get clumping and you'll need to stop the mixer and scrape mix off the back and perhaps the paddles to avoid clumps of dry premix. It's not onerous, but it will happen, so don't forget this step. I often use a chunk of 2x4 as a scraper.
Frankly, it's best if you measure the actual amount of water needed. This is most easily done with a container marked for the bags of premix you're using. Shoot for using the minimum-recommended amount of water, as this results in the strongest concrete.
Another tip is to not try pouring a bag of premix directly into the mixer. You'll find if you put half the bag into a 5 gallon bucket, it will be easier to put into the mixer. If I have a person helping, I'll ask them to use a fine fan spray on the nozzle to try to keep down the dust so we don't have to breathe it. Then dump in the other half of the bag using the bucket.
The typical 5 gallon bucket has a crummy handle for lifting heavy loads. Cut off the cheap plastic handle and make a new one by splitting a chunk of dowel and drilling a hole through it. Cut a groove near each end (put 2 or 3 hacksaw blades on a hacksaw frame) and secure the halves around the bucket handle's wire with some 1/16" braided nylon cord and a constrictor hitch. You will wonder why you didn't do this years ago.
A warning: be careful using the mixer in a wet location (i.e., standing water on the ground). I've done so at a neighbor's house and the extension cord for the mixer power went through the water and I got a slight tingle of a shock while using the mixer. The neighbor's outlet obviously didn't have a ground fault interrupter on its circuit as is required by modern electrical codes. Even better, bring an extension cord with a built-in GFI, as it will still protect you even if the outlet is ungrounded.
### Components
1. Add half of the needed water for the mix.
2. Add the gravel for this load.
3. Add the sand for this load.
4. Mix for 2 minutes.
  1. Note an advantage of doing things in this order is that the aggregates are scouring off any previously-mixed concrete.
5. Add the cement.
# Test cases
These are simple test cases that the program should successfully calculate.
## Cylinder
For a cylinder of diameter 2 m and length 1 m, the volume should be %pi `=` 3.14 " m"^3 .
## Slab
For a slab with all dimensions equal to 1 m, the volume should be 1 m3.
## Partial cylinder
For a horizontal cylinder of diameter 2 m and length 1 m that is filled to 50% of its height, the volume should be %pi/2 `=` 1.57 " m"^3 . For a percentage of 0, the volume should be zero.
## Sphere
A sphere of diameter 2 m has a volume of 4%pi/3 `=` 4.19 " m"^3 . For a sphere that is filled to 50% of the diameter of the sphere, the volume should be half of this or 2.09. For a percentage of 0, the volume should be zero.
# Premix or mix yourself?
You have two primary choices if you want to mix some concrete. You can use bags of premix, typically purchased in 60 lb and 80 lb bags. Or, you can buy the raw materials (cement, sand, and gravel) and mix things yourself.
A rule of thumb is that using the raw materials will cost you about 3 times less than the premix. The advantage of premix is the convenience of just opening up a bag and getting to work.
You'll probably want to use premix for small jobs and mix your own components for larger jobs. Here, you'll have to define "small" and "larger", but I would personally define a small job as something that takes no more than 10 to 20 bags of premix.
You'll also want to factor in the cost of transporting the materials.
Knowing what I know now, I wish I had taken the time years ago to build a storage area for sand and gravel. I would have made this on a concrete slab with concrete walls. Then I would have used some corrugated metal for a roof, with an eye to keeping the materials dry, probably by including some removable wooden doors. I would have stored cement powder in our outbuilding and been able to mix up needed concrete without having to drive to a store. In the last couple of decades, this foresight would have paid for itself many times.
The raw materials aren't very expensive and you'll find that having them immediately on-hand increases the number of projects you're likely to undertake.
# The concrete.py script
This is a python script, so you'll need to download and install python if you don't have it. It requires two python libraries, getnumber.py and sig.py, that were included in the concrete.zip file used for distribution. The script will prompt you for the following information:
1. Whether you're using premixed concrete or you want to mix your own cement, sand, and gravel.
2. The shape of the form you'll fill with the mixed concrete.
3. The dimensions of the form.
If you don't want to mess with a script, you can refer to the Pencil and paper calculations below to perform the calculations. They're not difficult at all -- and, in fact, with a little practice, you can do them without a calculator because you usually only need the answer to within around 10%.
The dimensions can be given in a number of different commonly-used units.
The script uses some internally-defined constants which you may wish to change. In particular, you may wish to change the following global variables
1. premix_yield_kg_per_m3
2. water_L_per_kg_of_concrete
3. strength_28_days_MPa
4. dried_components_scale_factor
Some of these variables contain numbers taken from the Quikrete 1101 datasheet, which is a common premix material sold in the US.
The easiest way to learn how to use the script is to run it. The following examples show two typical problems I might use the script for.
## Example premix problem
I wish to put in 8 fence posts. The posts are 4x4 material (actual size is 3.5 inches square) and the posts will be 2.5 feet in the ground. My post hole digger will dig an 8 inch diameter hole. How many bags of premix must I buy to mix the required concrete?
This problem needs to be solved by running the program twice. First, we find the number of bags of premix to fill 8 holes. Second, we find the number of bags of premix to fill the 8 4x4s. The answer is to subtract the second number from the first. You can think of it as we need to make an 8 inch diameter cylinder 2.5 feet long, then remove a volume equal to the 4x4.
Output of program
## Example with mixing raw materials
I have a 45 m section of fence that I wish to put a 1 foot wide concrete strip 3 inches thick under to provide a barrier and prevent weed growth[1]. How much sand, gravel, and cement should I buy to mix the concrete for this strip?
[1] I'm intentionally mixing up the units to show the script can handle the mix.
## Dealing with holes
  10x13 Glenda Guard forms, 4.5" OD pipe, form has 3 slots

# Text
Good basic reference:
http://www.motherearthnews.com/diy/using-cement-zmaz88jazgoe.aspx

The generally-accepted volume mixture ratio for concrete is:

    Cement 1
    Sand 2
    Gravel 3 to 4

    A key is to get the correct amount of water. Shoot for 0.3 to 0.5 mass ratio of water to cement.

Another recipe:

    1 shovel of cement
    2 shovels of sand
    3 shovels of small rock mixture (not rounded pebbles, but rocks
        with sharp corners)

For a mortar or cement with only sand, the mixture is:

    Water 1
    Cement 2
    Sand 3

    Add some hydrated lime to make it more workable and
    more moisture-resistant.

Hydration: for a unit of mass of concrete m, you need a mass of m/4
of water to hydrate the concrete. However, a mix with a 0.25 may be
hard to place, so sometimes a 0.4 to 0.5 ratio is used. To use a mix
closer to the 0.25 ratio, use a plasticizer.

From the Quikrete 1101 data sheet, an 80 lb bag of premix results in
0.60 cubic ft of concrete. It takes 2.8 liters of water.

Mix the dry contents thoroughly, then add the water. Mix about 75% of
the water first, then slowly add the remaining amount, mixing things
thoroughly. You'll quickly get a feel for the right stiffness of the
mix. Note: the best mix is probably stiffer than you think,
especially if you haven't mixed concrete before. The best thing you
can do is a slump test (see below) to ensure correct mixing.

You have roughly 30-45 minutes to work (spread, tamp, & level) with
the concrete after it is mixed. It will harden in about an hour, be
half strength in about 3 days, and be full strength after about a
month. These numbers depend on the ambient temperature.

From http://en.wikipedia.org/wiki/Water%E2%80%93cement_ratio:

    Too much water will result in segregation of the sand and
    aggregate components from the cement paste. Also, water that is
    not consumed by the hydration reaction may leave the concrete as
    it hardens, resulting in microscopic pores(bleeding) that will
    reduce the final strength of the concrete. A mix with too much
    water will experience more shrinkage as the excess water leaves,
    resulting in internal cracks and visible fractures (particularly
    around inside corners) which again will reduce the final strength.

    The 1997 Uniform Building Code specifies a maximum 0.50
    water-to-cement ratio (1:2) when concrete is exposed to freezing
    and thawing in a moist condition or to de-icing chemicals, and a
    maximum 0.45 water to cement ratio for concrete in severe or very
    severe sulfate conditions.

Slump test: use a tapered Styrofoam cup. Pack the concrete into the
cup. Remove the cup vertically. The ideal is for the pile to slump
to about 30-50% of its original height. More has too much water. Less
will be harder to work.

Use as large an aggregate as you can to save money, up to 2". The
stones should be no larger than 1/4 of the thickness being poured.

It takes about 1.5 volumes of dry mix to make 1 volume of mud.

Always make a trial mix, then keep records to help you make the same
mix in the future.

It's best to measure by mass, but virtually all homeowners &
do-it-yourselfers do it by volume.

If you live in a cold environment, add an air-entraining agent to the
mix. This agent also improves the workability of the concrete. If
you're mixing you're own, buy a bag of 1A Portland cement, as it has
the agent mixed in.

One 80 lb bag of premix = 2/3 cubic foot
1 bag of cement = 88-93 lbs. Mixes with 5 gallons of water.
1 gallon water = 8.3 lb
1 cubic foot:
    sand/gravel = 85-100 lbs
    plain concrete = 140-150 lbs
    water = 62-65 lbs
2 cubic foot:
    6 sq ft slab 4" thick
    8 sq ft slab 3" thick
1 cubic yard:
    80 sq ft slab 4" thick
    108 sq ft slab 3" thick

Using a mixer:

    Add in about 1/2 the water first. Then cut open bags of premix
    and add half to a 5 gallon bucket. This makes it easier to pour
    into the mixer.

    Mortar: if you are not using premixed, put the sand in first then
    the lime and cement.

Mixer process:

    - In the Harbor Freight mixer I have, it's easiest to mix one 80
      lb bag of premix at a time (2/3 cubic feet of concrete). I
      believe the mixer, however, is rated to mix 1 cubic foot at a
      time. It will probably do a bit more. (Actually, it's probably around 3 ft3.)

    - Put roughly 1/2 the water needed into the mixer, then add the
      premix and start mixing. You'll want to stop it a few times and
      inspect for places in the mixer where it is clumping. I use a
      stick to break the clumps loose.

    - Add a little water at a time and let it mix some more. There's
      a relatively clear point you reach where it looks about right.
      If you see it smoothly flowing around the mixing paddles as if
      it was a heavy mud, you've added too much water.

    - Prepare the place you'll put the concrete thoroughly. Make sure
      it's damp (not muddy) before you pour the concrete mix.

    - When it looks right, dump it into a bucket or wheelbarrow and
      take it to the job. Shovel it in if possible rather than
      dumping it all in at once, as this lessens the possibility of
      voids.

    - The tamping step is very important. Add about 3" of concrete,
      then tamp. One step of tamping is with a steel rod; your goal
      is to compress the aggregate a bit and remove any air pockets.
      Then compress with something like a 4x4 to tamp things down
      better. Repeat with another 3" layer until you get the desired
      thickness.

    - Cover up the concrete with hay or plastic sheet. If you use
      hay, wet the concrete at least two times a day for the next few
      days (perhaps 3 days; in really hot weather, do this for about 5
      days). If you use plastic, inspect the plastic to verify there
      is moisture on the underside of the plastic. If not, spray a
      little water on the concrete and cover it back up.

## 80 lb premix = 0.6 cubic feet
This relationship can be calculated knowing some basic numbers. The specific gravity of cured concrete is between 2.3 and 2.5. This is in g/cc or Mg/m3 (some people will use[2] tonne/m3, but I dislike seeing multiple mass units used -- use either kg or g). Let's use 2.4 g/cc, which is equivalent to a concrete density of 150 pounds mass per cubic foot, a commonly-seen number.
[2] A tonne is 1000 kg.
To calculate the volume of this mass of concrete, divide by the density in pounds per cubic foot: (80 "lbm")/(150 "lbm/ft"^3) `=` 0.53 "ft"^3 . Hmm, that's not the same as the 0.6 ft3 the product says it will do. The difference is that we didn't include the mass of the water.
Suppose the bag was mixed with 3 liters of water, slightly over the minimum recommended 2.8 liters of water. This would be a mass of 6.6 pounds. Then the volume calculation would be 86.6/150 or 0.58 cubic feet. Thus, you can see about where the 0.6 ft3 number comes from.
## Pouring
The most common mistake beginners make is to add too much water to the concrete. Too much water results in
- Reduced final compressive strength. Water that is not consumed by the hydration reaction may leave the concrete as it hardens, resulting in microscopic pores (bleeding).
- Concrete that is more likely to crack.
- Surface water after finishing, which can lead to flaking and be unsightly.
- Segregation of the sand and aggregate components from the cement paste.
- More shrinkage as the excess water leaves, resulting in internal cracks and visible fractures (particularly around inside corners) which will reduce the final strength.
For good results, measure the proper amount of water to get a 0.45 water to cement mass ratio.
[cr] The 1997 Uniform Building Code specifies a maximum 0.50 water-to-cement mass ratio (1:2) when concrete is exposed to freezing and thawing in a moist condition or to de-icing chemicals, and a maximum 0.45 water to cement ratio for concrete in severe or very severe sulfate conditions.
A practical technique is to check your concrete mix is to use a slump test (see the section Slump test below). Using a tapered Styrofoam cup, pack the concrete into the cup. Remove the cup vertically. You should probably shoot for the pile to slump to about 30-50% of its original height. Less height (more slumping) means the concrete has too much water. Less slumping will be harder to work.
It's best to pour concrete in moderate temperatures; typical is 50 to 90 °F. Pouring in temperatures outside this range can require extra steps; consult the web for details.
You should transport the mixed concrete to the form in a bucket or wheelbarrow. Make sure the bottom of the form is damp (not muddy). If possible, shovel the concrete into the form rather than dumping it all at once to reduce the chance of voids forming. Shoot for adding about a 3 inch thick layer and tamping this layer. Then add another layer if needed.
After you've placed the concrete, you'll want to tamp it to remove voids and settle things. Use a chunk of rebar, dowel, or steel pipe with its end plugged. Once that tool has thoroughly tamped the concrete, you can use something like a 4x4 on end to tamp the surface down a bit more.
After tamping, you can delay for a bit and then finish the surface of the concrete by floating, troweling, etc. I'll let you research this part on the web, as there are a variety of techniques.
A key number to keep in mind is that you have approximately an hour after mixing to do something useful with the concrete. After that amount of time, it may be too hard to work.
Cover up the concrete with hay or plastic sheet while letting it cure. If you use hay, wet the concrete at least two times a day for the next few days (perhaps 3 days; in really hot weather, do this for about 5 days). If you use plastic, inspect the plastic to verify there is moisture on the underside of the plastic. If not, spray a little water on the concrete and cover it back up. Keeping the atmosphere over the concrete saturated with moisture while it's curing will help avoid cracking and get the best cure.
# Slump test
A slump test can be used to establish the suitability of mixed concrete. The idea is to fill a tapered container with the mixed concrete, then invert it and lift the container off. The concrete will slump down; the amount of slump is an indication of the quality of the mix.
You can use a Styrofoam or tapered plastic kitchen cup. The national and building standards specify a frustum of a right circular cylinder which is 4 inches diameter at the top, 8 inches at the bottom, and 12 inches long (it's called an Abrams cone). This is a portion of a cone with a sidewall that is tapered tan-1((8 - 4)/(2*12)) or 9.5° with respect to the longitudinal axis of symmetry. Here are the dimensions in inches of some tapered cups I measured in our home:
Though these cups aren't the requisite angle of the standard, you'll find they're suitable approximations.
You should put a third of the concrete into the cup, then tamp it in with a steel rod or wooden dowel (about 1/2 to 3/4 inch in diameter -- a piece of 1/2 inch rebar is just right). The tamping is important to eliminate voids. Add another third and re-tamp. Finally, add the last third and re-tamp. Then screed off the top level with the top of the cup. Try to emulate the tamping you'll use with the real concrete pour. Turn the cup over on a non-porous surface and lift the cup straight up. Assess the slump by the following picture:
The change in height from the cup's overall height to the slumped-pile's height is the slump measure. A collapsed slump means the concrete is too wet. A shear slump indicates that you should get a new slump sample. The true slump is what you want. I'll let you research the measurement and interpretation details on the web; you'll decide what is appropriate through some experience.
The slump test is useful because it is quantitative and evaluates the workability of the concrete.
# Pencil and paper calculations
This section shows in detail how you'd solve the two types of problems using just pencil and paper. Note it's appropriate to work to two significant figures and round up by 10% or so at the end to be practical. I'll re-solve two of the problems given above.
These calculations are often done on a piece of scrap wood outside while you're working, so it's appropriate to only use approximations. If you're unfamiliar with these types of calculations, you can refer to the DinosaurArithmetic.pdf document at http://code.google.com/p/hobbyutil/ for more information.
I do have one caution, however. It can be expensive (time, money, work, rework) to make a mistake in performing these calculations blindly and not using your common sense/experience in evaluating the result. Here's an example. Suppose you want to make a concrete slab 4 feet by 8 feet by 3 inches thick. You convert the feet to inches and calculate the volume in cubic inches as 48(96)(3/12) . You approximate this as 50(100)/4 or 5000/4, which is 1250 cubic inches. To convert this to cubic feet, you divide by 123 = 729 to get a bit less than 2. But 2 cubic feet doesn't sound right, as it seems low from experience (this is a slab the size of a 4'x8' sheet of plywood). Do the calculation in feet:
{4 cdot 8 cdot 3 over 12} `=` 8
Of course, you immediately see the problem -- you accidentally converted the 3 inches to feet in the cubic inch calculation. The lessons are 1) to use your common sense and experience to evaluate the resulting volume or bags of concrete and 2) repeat the calculation in different units. Both can uncover "dumb" mistakes that we all make from time to time.
If you can use a computer, use the wonderful GNU units program to do these calculations. Here's one way to calculate the above problem:
You have: 4 ft 8 ft 3 in bag80
You want:
        Definition: 13.3333
This is because 8 cubic feet will require 0.6 bags of premix per cubic feet, or 13.3 bags. We get the same results calculating in inches:
You have: 48 96 3 in3 bag80
You want:
        Definition: 13.3333
To be able to do such calculations, I modified my units.dat file with the following lines to let me calculation in premix bags:
# Bags of Quikrete concrete (number of bags per cubic foot)
bag80 1/0.6 ft3 # 80 lb bag
bag60 1/0.75 0.6 ft3 # 60 lb bag
## Premix problem
The problem is:
I wish to put in 8 fence posts. The posts are 4x4 material (actual size is 3.5 inches square) and the posts will be 2.5 feet in the ground. My post hole digger will dig an 8 inch diameter hole. How many bags of premix must I buy to mix the required concrete?
We'll work in units of feet.
The hole is 8/12 or 2/3 feet in diameter and 2.5' long, so the volume of this cylinder is the area of the cylinder multiplied by the cylinder's length: left (%pi(2/3)^2/4 right ) 2.5 `=` 0.87 " ft"^3 .
If you don't have a calculator handy, you approximate the problem as follows:
{22 over 7} cdot {4 over 9} cdot {1 over 4} cdot {5 over 2} `=` {22 cdot 5} over {7 cdot 9 cdot 2} `=` {11 cdot 5} over {7 cdot 9} `=` 55 over 63 `=` 0.9
because you can see that 0.9 of 63 is only slightly more than 55. In fact, it's about 4% high, so you can subtract 0.04 from 0.9 to get 0.86 (but I'd use the 0.9 because it estimates a little high).
We have to subtract off the volume of the 4x4, which is 2.5(3.5/12)2 or 0.21 ft3.
Again, if you don't have a calculator, you approximate the problem as follows. 3.5 is 7/2 and squaring that gives 49/4. That's just slightly over 48/4 or 12. Hence, the squared term in parentheses is equal to 1/12. The result is (5/2)/12. Since you know 1/12 is about 0.08 (i.e., slightly less than 0.1), we get 0.4/2 or 0.2.
Thus, the hole volume is about 0.7 ft3 and eight holes will require 5.6 ft3. Since an 80 lb bag provides 0.6 ft3 of cured concrete, we need 56/6 or 9.3 bags. We'll buy 10 bags and have a little left over for contingencies.
Since an 80 lb bag of premixed concrete uses 2.8 liters of water, I'll need 9.3(2.8) or 26 liters of water (this is 6.9 gallons).
## Raw material problem
A standard #2 shovel's volume is given by the rule of thumb that a cubic yard takes 150 shovel loads. This gives the shovel's volume at 5.1 liters (5.1×10-3 m3), 1.35 gallons, or 0.18 ft3. (I usually use the rule of thumb that 5 shovels are needed to produce 1 cubic foot.) Clearly, to do reasonably careful work, measure the shovel's volume yourself with the materials you plan on working with.
Let's suppose we want a slab of 1 cubic foot -- and this is the volume of the cured concrete.
The first rule of thumb used is that one increases the finished concrete volume to get the required volume of dry components. This is because when the dry components are mixed with the water, the particulates can get in closer contact. Thus, multiply the desired concrete volume by 1.5.
We need 1.5 cubic feet of dry mixed. Since the most-commonly-used volume ratio of cement to sand to gravel is 1:2:3, we have that the required cement volume is 1(1.5)/6, the sand volume is 2(1.5)/6, and the gravel volume is 3(1.5)/6. Thus, the needed volumes in cubic feet are

## Calculation of water required
Define
size 14 bold {%alpha ``=`` "water to cement mass ratio"} .
The stoichiometric amount of water required for the strongest concrete is  = 0.25. There are two problems with this value. First, it will result in a difficult-to-work and stiff mixture. Second, we homeowners always measure components by volume, not by mass. Thus, if I had put in three shovels of cement, how much water should I add?
Aside: a practical way to solve this problem would be to measure the mass M of a shovel of cement. Then it's easy to calculate the required amount of water: each kg of cement mass needs M liters of water. If you standardize on e.g.  = 0.45, then you can make a container with needed mass of water. This would be a preferred way of mixing cement until it "looks right", unless you're very experienced.
What's the density of cement? A 90 pound bag of cement is 1 cubic foot. Using the GNU units program, this translates into a specific gravity of 1.44 g/cc. Glover, Pocket Reference, Sequoia Publishing, 1993, gives it as 1.60. Other references I have give up to 3.2 g/cc. Which is correct? The problem is caused by the fact that the cement is a powder and the density will obviously depend on how it is compacted. The 3.2 g/cc is for a densely-packed powder. The 1.44 g/cc value is for the cement in the bag. If you've ever shoveled from a bag, you know that some air will get entrained with the cement, so even the 1.44 g/cc is probably a bit high for practical mixing. The best thing you can do is measure the density of the cement as you normally use it. If you don't have a way to measure mass, then you'll have to assume a specific gravity. I've used 1.4 g/cc in the script.
We can make some estimates from the Quikrete 1101 data sheet. For an 80 pound bag, the manufacturer recommends adding 2.8 L (3/4 gal) of water, and allows you to go up to 4.3 L (1.1 gal) maximum. If we assume this mix uses the usual 1:2:3 ratio of cement:sand:gravel, then this means the bag contains 80(1/6) or 13.3 lb = 6.05 kg of cement. For an  of 0.25, this would mean a volume of 1.5 L of water (this is why you convert to kg, as a kg of water is 1 L). Thus, the 2.8 L recommended minimum means an  of 0.25(2.8/1.5) or 0.46. You'll find  = 0.45 is a commonly-recommended value on the web. Using 4.3 L means an  of (4.3/2.8)0.46 or 0.71. I don't recommend using concrete quite that runny.
# Volumes
Here, I'll discuss a few common ways of measuring volumes when mixing concrete.
When I'm mixing components, my unit of measure is a shovel full of material.
## Volume box
A useful thing that's pretty easy to make is a box of known volume. A common thing in the US is to make a box with a volume of 1 cubic foot. Then you can count the number of shovels of material to fill the box, giving you a practical measurement of the shovel's volume. Most importantly, this is done with the materials you're using to mix concrete, so you can get the proper mixtures.
Here's one possible design of a volume box, using plywood of thickness t and some square material of size d to act as cleats to hold the wood screws:
The volume flush with the top is
size 12 bold stack { alignl V `=` {left [ (b - 2t)(a-t)c right ]} underbrace {"box volume"} - {4 d^2 (a - t)} underbrace {"cleat volume"} # alignl phantom V `=` (a - t) (b c - 4 d^2 - 2 c t) }
A bill of materials is:
Qty	Material	Location	Size
2	plywood	Left & right sides	a × b
2	plywood	Front & back	c × (a - t)
1	plywood	Bottom	b × c
4	stick	Cleats	d × d × (a - t)

I've read that commercial folks will often weld up a 1 cubic foot box from some steel sheet. This will be relatively simple to construct, be water-tight, and stand up to jobsite abuse.
## 5 gallon bucket
One of my favorite containers around the home is the 5 gallon bucket. These can be accurately calibrated in your favorite volume units (see the bucket.zip file at http://code.google.com/p/hobbyutil/). The usual bucket I use made by Rheem measures 5.64 gallons (21.34 L) when filled flush with the top.
Note the buckets have a slightly tapered shape so that they can be withdrawn from the plastic mold easily. You need to take this taper into account to calibrate the bucket; this is done by the python script given in the bucket.zip file. Once you figure out how to use it, this makes it easy to mark volume calibration marks on the outside or inside of your bucket with a tape measure. For concrete work, you can mark a hooked stick with 0 to 1 calibrations (with, say, 0.1 divisions) and measure things for mixing concrete with the bucket.
The concrete.py script assumes the bucket is cylindrical and gives the measure as a fraction of the bucket total internal height. You need to set the value of the global variables bucket_volume_L in liters and side_wall_taper_deg in degrees to have the script's output be relevant to the bucket you're using.
# Mass balance
If you can make or acquire mass standards, it's not too hard to make a mass balance suitable for mixing concrete. You can make the standards themselves from concrete and put handles on them for convenient use. If you want to work in pounds, the following set of standards could be suitable:
50, 50, 50, 20, 10, 10, 5, 2, 2, 1
These will let you construct any mass up to 200 pounds inclusive.
To work in kg, you might want to use
25, 25, 20, 10, 10, 5, 2, 2, 1
which will let you measure up to 100 kg.
In both cases, if you're willing to manipulate larger masses, you could e.g. replace the two 50 pound masses with one 100 pound mass and the two 25 kg mass with a 50 kg mass. I like to keep things around 50 pounds or less.
A suitable balance can be made from some plywood and 2x4s. The basic design is as follows
I'd suggest using a suitable level on the top of the pivot bar to indicate when the balance is in the balanced condition (or a conventional pointer can be used). A 2x4 is a likely pivot bar. A couple of 2x4s can be on either side of the bar and the pivot bar can pivot on a nail or bolt. Nothing needs to be terribly fancy. TM can be a tare mass used to adjust the zero reading of the scale.
I would make the plywood platforms wide enough to take a 5 gallon bucket for easy handling of the components. Keep a chunk of wood handy with the same mass as the bucket to tare it out or make the tare mass sufficiently heavy and adjustable to do this for you.
Since I have a lathe handy, I would make the pivot from a chunk of brass bar stock and have it mate with two brass flanges in the support. These brass flanges would be greased with axle grease and made to be a close sliding fit (within 0.001"). This would then be a robust scale that could be left outside in the weather. I would paint all the wood carefully to help protect it from moisture.
## Standards
Here's one design of a standard that I will probably use if I make such a scale and standards:
A is a rod welded to the top of B, a pipe cap. C is a pipe nipple encased in the concrete mass D. This provides both a handle to lift the mass and a cavity to add chunks of mass used to fine-tune the standard's mass.
You will probably want to make two identical standards of the smallest mass (e.g., 1 pound or 1 kg). You'd take these to a place that could measure their mass accurately and you'd adjust them to be the standard mass within a desired accuracy. These two standard masses can then be used to both check the balance and check the calibration of the other masses.
For the small masses, I would turn them from a relatively stable metal like brass or stainless steel (stainless steel preferred).
To check the balance, one of the 1 unit masses is put on either side of the scale. It should indicate balance. If not, the tare mass position is adjusted until balance is achieved.
Now the 2 unit masses can be checked against the two unit masses. Once two of those are checked and adjusted to be correct, they can be used to check the 5 unit mass. The remaining mass standards can be checked in a similar fashion.
If your balance is sensitive enough, you may want to make some sub-unit mass standards too.
# References
glover	T. Glover, Pocket Ref, Sequoia Publishing, 1993.
virg	http://www.virginiadot.org/VDOT/Business/asset_upload_file255_3529.pdf Good overview of the components of concrete.
memph	http://www.ce.memphis.edu/1101/notes/concrete/cylinder_concrete_mix_proportations.pdf
cr	http://en.wikipedia.org/wiki/Water–cement_ratio